# Material Marketing Terms vs Real Polymer Differences

Purpose: Separate branding language from actual material behavior so design decisions are based on chemistry, not hype.

Scope: Applies across PLA, PET-based materials, Nylon, and flexible filaments.
Not included: Scenario decisions, structural design, or feasibility conclusions.

## Why This Canvas Exists

Filament marketing frequently uses non-standardized terms that sound technical but do not correspond to regulated or industry-defined material classes. This canvas exists to: - Prevent false assumptions (“HT-PLA = high-temp plastic”) - Identify what claims are chemistry-backed vs branding-only - Reduce wasted prints and redesign cycles

## PLA Family – What the Names Really Mean

### PLA

- Base polylactic acid

- Low heat resistance

- Brittle compared to engineering plastics

This is a real polymer class.

### PLA+ / Tough PLA / Pro PLA / PLA Max

Marketing status: ❌ Not standardized

Typically indicates: - Impact modifiers - Plasticizers - Blend tweaks for printability

What it does not guarantee: - Higher heat resistance - Chemical resistance - Consistent mechanical improvement across brands

Two PLA+ filaments from different brands can behave very differently.

### HT-PLA (High-Temp PLA)

Marketing status: ⚠️ Conditionally meaningful

What it usually means: - PLA formulated for post-print annealing - Heat resistance improves only after controlled anneal

What it does not mean: - High-temperature performance as-printed - Equivalent to ABS, ASA, or Nylon

Design reality: - Without annealing, HT-PLA behaves like normal PLA - Annealing introduces shrinkage and warping risks

## PET-Based Materials – Real Chemistry, Loose Naming

### PET (Polyethylene Terephthalate)

- True base polymer (same family as soda bottles)

- Rare as pure consumer filament

### PETG

- PET modified with glycol

- Reduced crystallization → easier printing

This is a real polymer modification, but: - Chemical resistance varies by formulation - Heat resistance is still limited

### PETG+ / Tough PETG

Marketing status: ❌ Not standardized

Usually means: - Added flexibilizers - Printability tuning

Does not imply: - Oil or fuel resistance - Structural performance increase

## Nylon Naming – Mixed Reality

### True Nylon Designations (Real)

- PA6, PA66, PA12, PA610, PA612

- Governed by polymer chemistry

These have predictable tradeoffs (moisture, strength, stability).

### “Nylon” / “PA Blend” Filament

Marketing status: ⚠️ Vague

Could be: - PA6 + modifiers - PA12 blend - Copolymer nylon

Always verify: - Moisture sensitivity - Print temperature - Reinforcement (CF / GF)

## Flexible Filaments – TPU vs TPE

### TPU (Thermoplastic Polyurethane)

- Real polymer class

- Oil and grease resistant

- Defined by Shore hardness (e.g., 95A)

### TPE

- Broad category, not a single polymer

- Behavior varies widely

Hardness rating matters more than the name.

## Heat Claims – Common Misinterpretations

### Glass Transition (Tg) vs Usable Temperature

- Tg ≠ safe working temperature

- Load + time cause creep well below Tg

### “Withstands X°C”

Often means: - Short-term exposure - No load - Ideal lab conditions

## Food-Safe & Safety Claims (Preview)

### “Food-Safe Filament”

Almost always refers to raw pellets, not printed parts.

Printing realities: - Layer lines trap contaminants - No post-print certification

Design implication: - Use liners, inserts, or coatings - Treat printed parts as non-food-contact by default

## Key Takeaways

- Marketing terms are not material standards

- Only polymer designations (PLA, PA12, PETG) have real meaning

- Heat, chemical, and safety claims require context

- Scenarios decide whether a claim actually matters

## Where This Canvas Fits

- Supports Material Resistance – Quick Reference

- Feeds Scenario evaluations when claims conflict

- Prevents premature material assumptions