# Material Resistance – Quick Reference

Purpose: Fast, high‑level lookup while working scenarios.
Scope: Material behavior only — no designs, no feasibility conclusions.
Detailed decisions belong in Scenario canvases.

## PLA / PLA+

Heat - Softens early; deformation can occur well below boiling water - Poor for warm environments or heat soak

Chemicals - Weak against petroleum products and solvents - Alcohol wipes generally tolerated briefly

Water - Stable in cold water - Hot water causes softening and creep

Mechanical - Rigid but brittle - Poor long‑term creep resistance under load

Notes / Best Use - Visual, low‑stress, indoor parts - Avoid heat, oils, fuels, long soaks

## PETG

Heat - Better than PLA but still creeps under sustained warmth - Not suitable for high‑heat soak

Chemicals - Tolerates water‑based cleaners - Marginal with oils and petroleum over time

Water - Good water resistance - Dishwasher / steam not recommended

Mechanical - Tough, flexible compared to PLA - Can creep under load

Notes / Best Use - General shop containers, guards, light enclosures - Avoid long‑term oil or solvent exposure

## TPU (95A)

Heat - Low heat tolerance - Softens and deforms easily

Chemicals - Generally resistant to oils and greases - Solvents can swell material

Water - Excellent water resistance

Mechanical - Flexible, impact resistant - Poor structural stiffness

Notes / Best Use - Gaskets, bumpers, vibration isolation - Not structural; not for sharp edges

## ABS

Heat - Good heat resistance - Better creep resistance than PETG

Chemicals - Resistant to many household chemicals - Attacked by some solvents

Water - Good water resistance

Mechanical - Tough, moderately flexible - Can crack under UV over time

Notes / Best Use - Enclosures, moderate‑heat shop parts - Indoor or protected outdoor use

## ASA

Heat - Similar to ABS with improved stability

Chemicals - Good resistance to oils and cleaners - Still not solvent‑proof

Water - Good water resistance

Mechanical - Tough and stable - Better long‑term performance than ABS

Notes / Best Use - Outdoor parts, sun exposure - Preferred ABS alternative when printing allows

## Nylon (PA – general)

Heat - Good heat resistance - Maintains strength under warmth

Chemicals - Excellent resistance to oils, fuels, greases - Variable solvent sensitivity by formulation

Water - Hygroscopic; absorbs moisture - Wet nylon changes dimensions and strength

Mechanical - Strong, tough, fatigue resistant - Can creep under constant load

Notes / Best Use - Functional mechanical parts - Requires drying and moisture control

### Nylon Designations (Quick Guide)

PA6 - High strength, high moisture absorption - Excellent oil and fuel resistance - Dimensionally unstable when wet - Harder to print

PA66 (Nylon 6,6) - Higher stiffness and heat resistance than PA6 - High moisture absorption - Rare as pure consumer filament - Often used in reinforced blends

PA12 - Lower strength, much lower moisture absorption - Very good chemical resistance - Best dimensional stability - Most printer-friendly nylon

PA610 / PA612 - Balanced strength and stability - Lower moisture absorption than PA6/66 - Excellent chemical resistance - Good long-term performance

PA-CF / PA-GF (Filled Nylons) - Much stiffer, lower creep - Reduced warping - More brittle than unfilled PA - Abrasive; hardened nozzle required

## HDPE / PP (Non‑Printed Liners / Inserts)

Heat - Moderate heat tolerance - Not structural at elevated temps

Chemicals - Excellent chemical resistance - Suitable for petroleum and solvents

Water - Excellent

Mechanical - Flexible, low stiffness

Notes / Best Use - Liners, inserts, chemical containment - Pair with printed structure for hybrid designs

## Conventions

- Keep this canvas short and scannable

- Use scenario canvases for decisions

- Structural design guidance lives elsewhere

## Topics to Cover Later (Backlog)

(High-level placeholders — to be expanded only if/when needed)

### Material Designations & Naming

- PLA variants: PLA, PLA+, Tough PLA, HT-PLA (what is chemistry vs marketing)

- PET-based materials: PETG, PET, PETT, PETG blends

- Nylon blends: how “PA blend” labels differ from true PA designations

- Elastomer naming: TPU vs TPE vs hardness ratings (e.g., 95A)

### Marketing vs Real Specifications

- What terms are not standardized (PLA+, Tough, Pro, Max)

- How to identify genuine material differences vs brand hype

- What properties are commonly exaggerated (heat resistance, food safety)

### Heat-Related Claims

- HT-PLA: annealing-required vs true high-temp polymers

- Glass transition (Tg) vs real-world usable temperature

- Short-term vs sustained heat exposure claims

### Standards & Regulations

- Are there industry-wide specs for filament materials? (short answer: mostly no)

- Relevant standards bodies:

  - ASTM / ISO material definitions (raw polymer level)

  - FDA / EU food-contact regulations (raw material vs printed object)

- Why filament labels rarely equal certified end-use parts

### Food-Grade & Safety Claims

- “Food-safe” filament vs food-safe finished part

- Raw material certifications vs FDM surface reality

- When coatings, liners, or inserts are required

- Pet safety considerations vs human food contact

### Additive & Modifier Effects

- Impact of fillers (CF, GF, mineral)

- Colorants and their effect on safety and heat

- Recycled vs virgin polymer claims

### Printing Reality vs Datasheets

- Layer adhesion as a failure mode

- Porosity and wicking in chemical exposure

- Why real-world performance deviates from spec sheets

(Each topic above should become its own focused canvas only if it proves useful in real scenarios.)