# Bambu Studio – Advanced Surface Quality (Flat vs Curved Surfaces)

Overview

This article explains the deeper mechanics behind improving surface quality in Bambu Studio, focusing on the differences between flat and curved surfaces.

1. Why Curved Surfaces Look Rough

FDM printers build objects layer by layer, which creates a stair-stepping effect on curves. This is the primary reason curved surfaces appear rough compared to flat tops.

2. Flat vs Curved – Fundamental Difference

Flat surfaces are controlled by top-layer behavior, while curved surfaces are controlled by layer height resolution.

Flat = Top layers + surface finish settings

Curved = Layer height + geometry resolution

3. Layer Height and Its Impact

Lower layer heights reduce visible stepping on curves.

Typical comparison:

0.20 mm – noticeable stepping

0.16 mm – moderate improvement

0.12 mm – smooth

0.08 mm – very smooth but slower

4. Adaptive Layer Height

Adaptive layers dynamically reduce layer height on curves and increase it on vertical walls.

Benefits:

- Better curves without major time increase

- Optimized print efficiency

Limitations:

- Can introduce inconsistencies on some geometries

- May slightly affect visual uniformity

5. Top Surface Quality Mechanics

Top shell layers build thickness above infill.

Topmost surface settings (speed, pattern, ironing) determine final appearance.

Important: These do NOT affect curved surfaces unless they become flat enough.

6. Speed and Cooling Effects

Curves often print slower due to geometry.

This can improve or degrade finish depending on cooling and extrusion consistency.

Outer wall speed has a strong impact on visible surface quality.

7. When Settings Interact

Common confusion comes from overlapping effects:

- More top layers improve flat surfaces but not curves

- Ironing only applies to flat surfaces

- Adaptive layers improve curves but don’t affect flat finishes

8. Practical Strategy

For mixed models (flat + curved):

- Use moderate layer height (0.16 or 0.12)

- Enable adaptive layers

- Tune top surface settings separately

- Use modifiers if only certain areas need higher quality

9. Key Takeaway

Flat and curved surfaces are governed by different mechanics.

Trying to fix curves with top-surface settings will not work.

Focus on layer height for curves and surface settings for flats.